## Slide 1
Carbon-decorated divacancies in hBN
First-principles screening toward UV–VIS quantum emitters
Status report and project roadmap for FTMC discussion
Franciszek Zabierowski
Warsaw University of Technology
FTMC discussion: Lukas Razinkovas group

## Slide 2
What this presentation is about
Franciszek Zabierowski | FTMC project discussion
Scientific question
Can carbon-decorated divacancies form optically active centers in hBN?
Do they create localized in-gap states suitable for UV–VIS emission?
Which geometries are worth full optical-property calculations?
What is done
Defect-nomenclature scheme and structural models
PBE → HSE relaxation workflow
Neutral-state calculated in HSE
Excited-state geometries
What remains
ZPL, Huang–Rhys factor, Debye–Waller factor, PL lineshape
Optical matrix elements and final candidate ranking
Charge-transition levels to justify q = 0 optical calculations
Complete ΔSCF / excited-state convergence

## Slide 3
Motivation: hBN emitters are promising, but their microscopic origin is often unclear
Franciszek Zabierowski | FTMC project discussion
Why hBN?
Wide-bandgap van der Waals material
Room-temperature single-photon emission has been observed
Emitter classes span UV, blue, visible and NIR ranges
2D geometry makes integration with nanophotonics attractive
The bottleneck
Many emitters remain chemically unidentified
Carbon is repeatedly implicated in UV/VIS emission
Different local geometries may yield very different spectra
DFT is needed to connect structure, levels and optical fingerprints
Project position
This project focuses on carbon-decorated divacancy complexes as a bridge between two known motifs:
  carbon dimer
  divacancy
The target is not only “does it emit?”, but also “which local bonding topology controls the emission?”
Context: Aharonovich et al., Nano Lett. 2022; Çakan et al., Adv. Optical Mater. 2025

## Slide 4
Two reference motifs: carbon dimer and BN divacancy
Franciszek Zabierowski | FTMC project discussion
carbon dimer
Calculated ZPL ≈ 4.31 eV
Experimental ZPL = 4.08 eV band
Huang–Rhys factor S ≈ 2
Radiative lifetime ≈ 1.2 ns
Transition between localized p-type defect states (https://doi.org/10.1063/1.5124153)
My calculations: ZPL = 2*5451.117 - 5451.566 - 5454.872 = 4.20 eV
My calculation:

## Slide 5
Two reference motifs: carbon dimer and BN divacancy
Franciszek Zabierowski | FTMC project discussion
Calculated ZPL ≈ 4.31 eV
Experimental ZPL = 4.08 eV band
Huang–Rhys factor S ≈ 2
Radiative lifetime ≈ 1.2 ns
Transition between localized p-type defect states (https://doi.org/10.1063/1.5124153)
My calculations: ZPL = 2*5451.117 - 5451.566 - 5454.872 = 4.20 eV
My calculation:

## Slide 6
Two reference motifs: carbon dimer and BN divacancy
Franciszek Zabierowski | FTMC project discussion
V₂ = divacancy
Divacancies are probable in irradiated hBN
Reconstruction yields 5–8–5 topology
Characteristic strong B–B and N–N bonds
Migration barriers: single-step divacancy motion in Zobelli et al.
Zobelli et al., Phys. Rev. B 2007, DOI: 10.1103/PhysRevB.75.094104
Bond B-B: 1.931 vs 1.93 (Zobelli)
Bond N-N: 1.681 vs 1.74 (Zobelli)
Activation energy for vacancy migration: 1.4eV – 1.8eV (Zobelli)
Can be created by electron irradiation (Zobelli)

## Slide 7
Defect construction and nomenclature
Franciszek Zabierowski | FTMC project discussion
Notation used here
B atoms: green; N atoms: blue; C atoms: black
V₂ denotes the reconstructed BN divacancy
“dimer” denotes isolated substitutional
Labels such as 2–3 or 4–6 denote the two carbon positions around V₂
All structures shown here are neutral unless explicitly stated otherwise

## Slide 8
Computational setup
Franciszek Zabierowski | FTMC project discussion
Model
hBN supercell: 8 × 8 × 2
Γ-point sampling
Neutral charge state q = 0
Spin-polarized calculations: ISPIN = 2
ENCUT = 500 eV
Calculated = 5.914
All candidates first relaxed in PBE
HSE relaxation after PBE pre-relaxation
HSE parameters:
  HFSCREEN = 0.2
  AEXX = 0.31
Van-der-Waals interactions taken into account using GrimmeD3 approach:
  IVDW = 11
  S6 = 1.000
  S8 = 0.722
  SR = 1.217
Functional strategy
Excited states
ΔSCF-like constrained occupations using FERWE / FERDO
Excitation defined as electron transfer between selected defect levels
Excited-state geometries partially converged; several remain problematic
Triplet single-point energies via NUPDOWN = 2 where needed
First relacation in PBE
Final geometry in HSE for ground state
Excited state geometry in PBE for approximation
Excited state in HSE
Tryplet energy for excited state geometry
Ground state energy for excited state geometry

## Slide 9
Optical-property model: what the next calculations will deliver
Franciszek Zabierowski | FTMC project discussion
Energy quantities
Ground-state minimum:
Excited-state minimum:
Vertical absorption:
Vertical emission:
ZPL:
Project-specific spin-correction route under discussion:
where is obtained as NUPDOWN = 2 at with NSW = 0.

## Slide 10
Current numerical summary: relative energy and structural reorganization
Franciszek Zabierowski | FTMC project discussion
defect | [eV] | [eV] (PBE) | [eV] (HSE) | ZPL [eV] | / | DW
 |  | --- | 0.209 | 4.2 | 1.97/2.06 | ---
 | 0 | --- |  | --- | --- | ---
1–2 | 0.541 | 2 | --- | --- | --- | ---
2–3 | 2.491 | 0.478 | 0.698 | --- | --- | ---
2–6 | 1.783 | --- | --- | --- | --- | ---
3–4 | 2.089 | 0.860 | --- | --- | --- | ---
3–8 | 3.903 | 0.460 |  | --- | --- | ---
4–5 | 1.213 | 0.375 | 0.417 | --- | --- | ---
4–6 | 2.150 | 0.352 | 0.380 | --- | --- | ---
4–9 | 1.842 | 0.926 | --- | --- | --- | ---
6–7 | 1.131 | 0.172 | 0.220 | --- | --- | ---
defect |  |  |  | ZPL [eV] |  | DW
 |  | --- | 0.209 | 4.2 | 1.97/2.06 | ---
 | 0 | --- |  | --- | --- | ---
1–2 | 0.541 | 2 | --- | --- | --- | ---
2–3 | 2.491 | 0.478 | 0.698 | --- | --- | ---
2–6 | 1.783 | --- | --- | --- | --- | ---
3–4 | 2.089 | 0.860 | --- | --- | --- | ---
3–8 | 3.903 | 0.460 |  | --- | --- | ---
4–5 | 1.213 | 0.375 | 0.417 | --- | --- | ---
4–6 | 2.150 | 0.352 | 0.380 | --- | --- | ---
4–9 | 1.842 | 0.926 | --- | --- | --- | ---
6–7 | 1.131 | 0.172 | 0.220 | --- | --- | ---
Interpretation used here: the V₂-referenced formation/binding-energy formalism cancels chemical-potential dependence. Δ_FC is treated as a proxy for structural relaxation/electron–phonon coupling strength.

## Slide 11
Geometry 1-2
Franciszek Zabierowski | FTMC project discussion
Lack of convergance in PBE and HSE in excited state
Franck-Condon shift already large (>2eV) (PBE).
Further calculations are abandoned

## Slide 12
Geometry 2-3
Franciszek Zabierowski | FTMC project discussion
defect | [eV] | [eV] (PBE) | [eV] (HSE) | ZPL [eV] | S | DW
2–3 | 2.491 | 0.478 | 0.698 | --- | --- | ---
defect |  |  |  | ZPL [eV] | S | DW
2–3 | 2.491 | 0.478 | 0.698 | --- | --- | ---

## Slide 13
Geometry 2-6
Franciszek Zabierowski | FTMC project discussion
defect | [eV] | [eV] (PBE) | [eV] (HSE) | ZPL [eV] | S | DW
2–6 | 1.783 | --- | --- | --- | --- | ---
defect |  |  |  | ZPL [eV] | S | DW
2–6 | 1.783 | --- | --- | --- | --- | ---
Lack of convergance in HSE and PBE for excited state
VASP is changing the order of orbitals

## Slide 14
Geometry 3-4
Franciszek Zabierowski | FTMC project discussion
defect | [eV] | [eV] (PBE) | [eV] (HSE) | ZPL [eV] | S | DW
3-4 | 2.089 | 0.860 | --- | --- | --- | ---
defect |  |  |  | ZPL [eV] | S | DW
3-4 | 2.089 | 0.860 | --- | --- | --- | ---
-5423.67339549 eV
-5424.33944231 eV
-5424.59162756 eV
-5423.67339549 eV
-5423.88315488 eV

## Slide 15
Geometry 3-8
Franciszek Zabierowski | FTMC project discussion
defect | [eV] | [eV] (PBE) | [eV] (HSE) | ZPL [eV] | S | DW
3–8 | 3.903 | 0.460 |  | --- | --- | ---
defect |  |  |  | ZPL [eV] | S | DW
3–8 | 3.903 | 0.460 |  | --- | --- | ---

## Slide 16
Geometry 4-5
Franciszek Zabierowski | FTMC project discussion
defect | [eV] | [eV] (PBE) | [eV] (HSE) | ZPL [eV] | S | DW
4–5 | 1.213 | 0.375 | 0.417 | --- | --- | ---
defect |  |  |  | ZPL [eV] | S | DW
4–5 | 1.213 | 0.375 | 0.417 | --- | --- | ---

## Slide 17
Geometry 4-6
Franciszek Zabierowski | FTMC project discussion
defect | [eV] | [eV] (PBE) | [eV] (HSE) | ZPL [eV] | S | DW
4–6 | 2.150 | 0.352 | 0.380 | --- | --- | ---
defect |  |  |  | ZPL [eV] | S | DW
4–6 | 2.150 | 0.352 | 0.380 | --- | --- | ---

## Slide 18
Geometry 4-9
Franciszek Zabierowski | FTMC project discussion
defect | [eV] | [eV] (PBE) | [eV] (HSE) | ZPL [eV] | S | DW
4–9 | 1.842 | 0.926 | --- | --- | --- | ---
defect |  |  |  | ZPL [eV] | S | DW
4–9 | 1.842 | 0.926 | --- | --- | --- | ---
-5423.60167078 eV
-5424.31766788 eV
-5424.41533639 eV
-5421.18710134 eV

## Slide 19
Geometry 6-7
Franciszek Zabierowski | FTMC project discussion
defect | [eV] | [eV] (PBE) | [eV] (HSE) | ZPL [eV] | S | DW
6–7 | 1.131 | 0.172 | 0.220 | --- | --- | ---
defect |  |  |  | ZPL [eV] | S | DW
6–7 | 1.131 | 0.172 | 0.220 | --- | --- | ---

## Slide 20
Current numerical summary: relative energy and structural reorganization
Franciszek Zabierowski | FTMC project discussion
defect | [eV] | [eV] (PBE) | [eV] (HSE) | ZPL [eV] | S | DW
 |  | --- | 0.209 | 4.2 | --- | ---
 | 0 | --- |  | --- | --- | ---
1–2 | 0.541 | 2 | --- | --- | --- | ---
2–3 | 2.491 | 0.478 | 0.698 | --- | --- | ---
2–6 | 1.783 | --- | --- | --- | --- | ---
3–4 | 2.089 | 0.860 | --- | --- | --- | ---
3–8 | 3.903 | 0.460 |  | --- | --- | ---
4–5 | 1.213 | 0.375 | 0.417 | --- | --- | ---
4–6 | 2.150 | 0.352 | 0.380 | --- | --- | ---
4–9 | 1.842 | 0.926 | --- | --- | --- | ---
6–7 | 1.131 | 0.172 | 0.220 | --- | --- | ---
defect |  |  |  | ZPL [eV] | S | DW
 |  | --- | 0.209 | 4.2 | --- | ---
 | 0 | --- |  | --- | --- | ---
1–2 | 0.541 | 2 | --- | --- | --- | ---
2–3 | 2.491 | 0.478 | 0.698 | --- | --- | ---
2–6 | 1.783 | --- | --- | --- | --- | ---
3–4 | 2.089 | 0.860 | --- | --- | --- | ---
3–8 | 3.903 | 0.460 |  | --- | --- | ---
4–5 | 1.213 | 0.375 | 0.417 | --- | --- | ---
4–6 | 2.150 | 0.352 | 0.380 | --- | --- | ---
4–9 | 1.842 | 0.926 | --- | --- | --- | ---
6–7 | 1.131 | 0.172 | 0.220 | --- | --- | ---
Interpretation used here: the V₂-referenced formation/binding-energy formalism cancels chemical-potential dependence. Δ_FC is treated as a proxy for structural relaxation/electron–phonon coupling strength.

## Slide 21
What remains to be done in Vilnius / next thesis stage
Franciszek Zabierowski | FTMC project discussion
Charge physics
Calculate charge-transition levels ε(q/q′)
Use them to justify focusing on q = 0 for optical calculations
Optical fingerprints
Compute ZPL consistently
Calculate Huang–Rhys factor and Debye–Waller factor
Generate CCD and PL lineshapes
Finish
Extended model space
Selected tetramers around V₂
Additional dimer positions: e.g. 3–9, 4–12
Same calculations for selected tetramers and other defects which carbon